## Slide 1
Effect of Washcoat Thickness
Thermal Modelling of Aerogel-Based Washcoats for Three-Way Catalytic Conversion: Effects of Washcoat Composition and Thickness on Light-Off Time
Allison M. Stanec1, Ian MacKellar1, Ann M. Anderson1, Mary K. Carroll2, Bradford A. Bruno1
Department of Mechanical Engineering1, Department of Chemistry2, Union College, Schenectady NY. USA
Project Objective and Goals
Future Studies / Recommendations
Although there are a number of challenges associated with using an aerogel-based washcoat, these results indicate that their use could reduce TWC light-off time. Finding a way to maintain the rapid temperature rise as the aerogel-based washcoat is first exposed to the exhaust gas would allow for even faster light-off.
It is evident that the aerogel properties enhance the heat transfer from the exhaust gas. Diffusion of heat through the washcoat is affected by the thermal diffusivity of the material, while the conductivity effects the penetration of heat via convection at the boundary. The next step is to better understand the relative importance of these material properties in reducing light-off time.
Conclusions
References
[1] Milton, B.E. (1998). Control Technologies in Spark-Ignition Engines, Handbook of Air Pollution from Internal Combustion Engines. Boston, MA: Academic Press.
[2] Burch, S., Potter, T., Keyser, M., Brady, M., and Michaels, K. (1995). Reducing Cold-Start Emissions by Catalytic Converter Management, SAE Technical Paper 950409.
[3] Nelson, J. (2009). Catalytic Converter and Functions [Online Image]. Wikimedia Commons. https://commons.wikimedia.org/wiki/File:Catalyticconverter.jpg
[4] Zhu, Y., Lv, G., Song, C., Li, B., Zhu, Y., Liu, Y., Zhang, W., and Wang, Y. (2019). Optimization of the Washcoat Slurry for Hydrotalcite-Based LNT Catalyst. Catalysts, 9(8), pp. 696. DOI 10.3390/catal9080696
[5] Joshi, S.Y., Harold, M.P., and Balakotaiah, V. (2009). Low-Dimensional Models for Real Time Simulations of Catalytic Monoliths. AlChE Journal, 55(7), pp. 1771-1783. DOI 10.1002/aic.11794.
[6] Sabatini, S., Kil, I., Dekar, J., Hamilton, T., Wuttke, J., Smith, M.A., Hoffman, M.A., and Onori, S. (2015). A New Semi-Empirical Temperature Model for the Three Way Catalytic Converter. IFAC Papers Online, 48(15), pp. 434-440. DOI 10.1016/j.ifacol.2018.10.031.
Acknowledgments
This project was funded by NSF grant IIP-1918217 and the Union College Summer Research fund. We would like to thank the Aerogel Lab group for the guidance and advice throughout the research.
Methods & Procedures
Data and Results
A large initial temperature rise is observed in the aerogel-based washcoats (Figs 4, 7). The temperature then levels off as the heat penetrates the cordierite layer (Fig 8).
A 20-µm-layer aerogel-based washcoat reaches light-off temperature 2-3 s faster than the alumina washcoat (an 8-17% decrease in light-off time). For a 100-µm-layer, the aerogel washcoats reach light off ~14 s faster (a 30% decrease in light-off time). See Fig 6.
Light-off time increases with washcoat layer thickness (Fig 6.)
If the overall wall thickness is kept the same, but thickness of the washcoat increases, the time to light-off for the aerogel washcoats is reduced by 28 s (300 cpsi) and by 16 s (400 cpsi) while the alumina washcoat light-off time only decreases by 0.7 s (Fig 7)
Similar trends were observed in the copper alumina and silica aerogel washcoats.
Although not shown, similar trends were observed for the 400 cpsi honeycomb; however, in all scenarios, the surface temperature of the 400 cpsi honeycomb reached light-off quicker.
A more realistic model with an exhaust temperature that increases with time showed similar results.
Background
Vehicle exhaust contributes to a significant amount of carbon monoxide (CO), nitrogen oxides (NOx) and unburnt hydro-carbons (HC) found in the atmosphere [2]. To reduce the pollutants released from automobiles, TWCs are used to enhance the reactions that convert harmful gases into less toxic gases through oxidation and reduction reactions. Catalytic converters are typically composed of an encased honeycomb ceramic structure covered with a catalyst washcoat (Figs 1, 2).
Typically, the washcoat is made from alumina impregnated with noble metal catalysts such as platinum, palladium and rhodium; however, these metals are rare and expensive.
The temperature at which there is a 50% conversion of the harmful gases is known as the light-off temperature.
Minimizing the time that it takes to reach the light-off temp-erature can significantly reduce pollutant emission.
A number of investigators have developed numerical models of catalytic converter performance; however, they are complex, and include both the heat and mass transfer that occurs in the converter. Joshi et al. [5] developed a model that generalizes the two-phase model and uses two modes at each axial position and includes heat and mass transfer between the solid channel and the exhaust. External heat and mass transfer coefficients are used based on previously developed correlations. Sebataini et al. [6] present a 1D temperature model that simulates the thermal dynamics inside the catalyst. Two sub-models are included: oxygen storage model and catalyst thermal model.
The goal of this work was to focus on the transient thermal behavior as the TWC heats up through the use of a finite difference heat transfer model.
L1 (µm) | 20
L2 (µm) | 150 (300), 75 (400)
Tinitial (K) | 300
Tinf (K) | 600
h (W/m2K) | 35
 | CuAl Aer. | Silica Aerogel | AlWC | Cordierite
k (W/mK) | 0.0567 | 0.02 | 2 | 1.5
ρ (kg/m3) | 100 | 100 | 2500 | 2600
cp (J/kgK) | 2070 | 1000 | 1000 | 1000
⍺ (m2/s) | 2.74E-07 | 2.00E-07 | 8.00E-07 | 5.77E-07
Figure 3: Channel wall model.
Table 2: List of input values used
Table 1: Material properties
300/400 cpsi Honeycomb Baseline Results
Effect of % Washcoat in the Wall Composition
Figure 1: A TWC showcasing the ceramic honeycomb structure [3]
Automotive three-way catalytic converters (TWCs) are used to reduce pollutant emissions. Upon an engine cold start there is a significant warm-up time prior to the TWC achieving "light-off" and becoming effective. This cold-start transient is a significant contributor to total pollution emissions [1].
Aerogels are nanoporous, thermally stable materials with a large surface area, low density, and low thermal conductivity.
The goal of this work is to assess the effect of an aerogel-based washcoat in place of the currently used denser and more thermally conductive alumina washcoat to determine if the use of aerogels can reduce the time needed to achieve light-off and decrease overall pollutant emissions.
A MATLAB-based transient 1D finite-difference heat transfer model was used to simulate the TWC channel walls in a 300 and 400 cells per square inch (cpsi) honeycomb structure.
The channel wall was composed of two materials: washcoat and cordierite (Fig 3) with the washcoat modeled as a copper-alumina (CuAl) aerogel-based washcoat, a silica aerogel-based washcoat or an alumina washcoat (AWC).
The left side of the model (the washcoat surface) was exposed to convection at 600 K, while the right side was modeled as a symmetry boundary.
A grid independence study was performed, and an Abaqus FEA analysis was used to verify baseline MATLAB results.
Figure 2: SEM image of a washcoat on a honeycomb wall [4]
Figure 4: Washcoat surface temperature versus time for a (a) 300 and (b) 400 cpsi catalytic converter.
Figure 7: Surface temperature for varying percentages of (a) CuAl and (b) AlWC for a 300 cpsi converter wall. Note: The total wall composition thickness for the 300 cpsi honeycomb is 170 µm. The aerogel-based washcoat shows a large initial temperature rise.
Figure 9: Temperature distribution of a 300 cpsi converter (150 µm cordierite) with an alumina washcoat at (a) 0.0001, (b) 0.001, and (c) 0.01 seconds. There is no distinct change in slope because the washcoat and cordierite have similar thermal properties.
Figure 8: Temperature distribution of a 300 cpsi converter (150 µm cordierite) with a CuAl washcoat at (a) 0.0001, (b) 0.001, and (c) 0.01 seconds. The cordierite layer begins at 0.425E-04, 0.85E-04, and 1.275E-04 m, for the 25, 50, and 75% washcoat, respectively. Note the slope change in the temperature profile as the heat penetrates the cordierite layer.
Figure 5: Surface temperature of (a) CuAl and (b) AlWC with varied washcoat thicknesses and a fixed cordierite thickness of 150 µm.
Figure 6: Light-off times for varied thicknesses of each washcoat. Large differences in light-off times are seen in the AlWC while small differences in light-off times are observed in the aerogel based washcoats.
 | CuAl | AlWC | Silica
Light-Off Time 300 cpsi (s) | 27.8 | 30.3 | 28.0
Light-Off Time 400 cpsi (s) | 14.1 | 16.9 | 14.1
Table 3: Light-off time for each washcoat for a 300 and 400 cpsi honeycomb.
Notes: The following describes example directions for a TRADITIONAL POSTER FORMAT (see next page for ALTERNATIVE POSTER FORMAT)
All posters are suggested to be 48-inches wide by 36-inches high, as used for this template.
Include the poster title, authors list, and affiliation(s). Use superscripts to annotate affiliation(s). The first author SHOULD be the presenting/registered student. Typically, a title font size is 72 pts with maximum of 3 lines.
Your abstract was assigned a 5-digit paper number. Insert the paper number (replace xxxxx) in the template toward the upper right corner below ASME logo. Moreover, please add the Poster Number (replace #), the Track Title (replace yyyy) and Track Number (replace Y), along with the Topic (replace zzzz) and Topic Number (Z).
Example sections are as follows:
  Project Objectives and Goals
  Background
  Methods & Procedures (can use “Experimental”, “Numerical”, or “Analytical” if desired)
  Data and Results
  Conclusions
  Future Studies / Recommendations
  Acknowledgements
  References
  The sizes of the section boxes can be adjusted as needed.
  Typically, heading fonts are Arial 44 pt and body text fonts are Arial 32 pt, except publication and reference lists in Arial 20 pt. Use large fonts so audience can read quickly and easily.
  Use illustrations and/or figures to help elucidate points and expand on the written material.